## Slide 2: Thermal Contact Conductance in Bolt Joints

## Slide 3
An expert is a man who has made all the mistakes which can be made, in a narrow field.

## Slide 4: Summary
Theoretical Heat flow
Real Heat Flow
Theoretical Models
Semi-Empirical Model
Empirical Model
Materials
Test Setup
Results
Discussion/Conclusion

## Slide 5: Theoretical Heat flow
Fourier Law of Heat Conduction
Multilayer Conduction
3 Dimensional
Unidimensional
Single Material Conduction

## Slide 6: Real Heat Flow
Surface Roughness
Force
Temperature
Microhardness
Oxide Layers
Thermal Constriction/Dilatation
Major Interface Parameters Affecting Conduction

## Slide 7
Theoretical Models
For:
Plastic: Modified CMY Model
Rocca Mikic Model for Bolted Joints
Elastic: Fletcher and Gyorog

## Slide 8: Semi-Empirical Model
Equivalent Fin Method (EFM)
Not suited for significative thermal conductivity variations.

## Slide 9: Empirical Model
Based on Empirical Joint Design
Rule of Thumb: Bolt Spacing for general construction should be at least 1,5 D to the edge and 4 D between bolts.
1.5 D
4 D
1.5 D
2 D

## Slide 10: Empirical Model
Step 1: Power Requirement Needed
Step 2: Estimate Temperature at the Joint

## Slide 11: Empirical Model
Inverted Flow
Radial Flow
Direct Flow
Perpendicular
Parallel
Step 3: Select Type of Joint
    Configuration (Parallel, Perpendicular, Inverted, etc…)

## Slide 12: Empirical Model
Step 4: Select Bolt Size
Step 5: Determine in Database Heat Transfer for Bolt Size, Material and Joint Temperature
Step 6: Divide Database Heat Transfer by Power Requirement to determine number of Bolts
Step 7: Validate Design

## Slide 13: Materials
44.01.30 - ALUMINIUM 99,5 % (EN AW-1050 A , state: H-24 half-hard)
44.09.56.B – COPPER (OXYGEN-FREE ELECTRONIC COPPER - Cu-OFE - EDMS 790780)
Tensile Strength | 200 to 240 MPa
Ultimate Strength | 240 to 280 MPa
Elongation at Break | 25% (min)
Hardness (Brinell) | 60 HBS (min)
Tensile Strength | 75 MPa (min)
Ultimate Strength | 105 to 145 MPa
Elongation at Break | 9%
Hardness (Brinell) | 38BH (min)
44.59.32.A - STAINLESS STEEL (304 L LOW CARBON) – EN 10088
Tensile Strength | 200 MPa
Ultimate Strength | 500 to 670 MPa
Elongation at Break | 45% (min)
Hardness (Brinell) | 192 BH (max)

## Slide 14: Test Setup
Heaters Protected with MLI
Three access ports available.
Two Wiring ports with 24 signal entries
(One for the PT100 probes) (24 used)
(One for Electric Power) (16 Used, 8 available)
Vaccum port can be modified to permit another 24 Signal entry
Radiation Shield
Cryostat

## Slide 15: Test Setup

## Slide 16: Test Setup

## Slide 17: Test Setup
All data presented for M4 A4-70 Stainless Steel Bolt, (Torque 3 N m), unless otherwise referred.

## Slide 18: Results: Cu-Cu
Chart: 
| 0.0 | 50.0 | 100.0
Teste 1A | 130.7 | 121.1 | 111.4
Teste 1B | 100.1 | 90.9 | 82.5
Teste 2A | 145 | 132.7 | 120.3
Teste 2B | 106 | 94.4 | 83.7
Teste 3A | 160.7 | 145.5 | 130.2
Teste 3B | 112.7 | 98.3 | 85.2
Teste 4A | 176.6 | 158.6 | 140.4
Teste 4B | 119.6 | 102.4 | 86.8
Teste 5A | 191.8 | 171 | 150
Teste 5B | 126.1 | 106.2 | 88.2
Teste 6A | 207.8 | 184 | 160.1
Teste 6B | 132.9 | 110.2 | 89.6
Temperature [K]
Distance [mm]
Very good linearity
Delta T with visible difference
Power transmitted (7 to 31W)
M4 A4-70 Stainless Steel Bolt, (Torque 3 N m)

## Slide 19: Results: Cu-Cu
Equation | Extrapolated Temperature [K] | Equation | Extrapolated Temperature [K] | Delta T [K] | Mean Joint Temperature [K] | Heat Power [W] | Conductance [W/K] | h [W/K m2]
y = -0,193x + 130,72 | 106,6 | y = -0,176x + 126,37 | 104,4 | 2,2 | 105,5 | 7,1 | 3,2 | 92420
y = -0,247x + 145,02 | 114,1 | y = -0,223x + 139,3 | 111,4 | 2,7 | 112,8 | 9,5 | 3,5 | 101506
y = -0,305x + 160,72 | 122,6 | y = -0,275x + 153,73 | 119,4 | 3,2 | 121,0 | 12,0 | 3,7 | 108232
y = -0,362x + 176,63 | 131,4 | y = -0,328x + 168,53 | 127,5 | 3,8 | 129,5 | 14,5 | 3,8 | 109469
y = -0,418x + 191,83 | 139,6 | y = -0,379x + 182,63 | 135,3 | 4,3 | 137,4 | 17,1 | 4,0 | 115404
y = -0,477x + 207,82 | 148,2 | y = -0,433x + 197,5 | 143,4 | 4,8 | 145,8 | 19,9 | 4,1 | 120150
y = -0,534x + 223,6 | 156,9 | y = -0,488x + 213,17 | 152,2 | 4,7 | 154,5 | 22,6 | 4,8 | 140242
y = -0,593x + 239,48 | 165,4 | y = -0,54x + 227,37 | 159,9 | 5,5 | 162,6 | 25,6 | 4,7 | 135891
y = -0,652x + 255,47 | 174,0 | y = -0,595x + 242,6 | 168,2 | 5,7 | 171,1 | 28,2 | 4,9 | 142781
y = -0,708x + 270,77 | 182,3 | y = -0,646x + 256,93 | 176,2 | 6,1 | 179,2 | 31,1 | 5,1 | 148556
Chart: 
| 11.30000000000001 | 14.3 | 17.49999999999999 | 20.80000000000001 | 23.90000000000001 | 27.19999999999999 | 30.19999999999999 | 33.39999999999998 | 36.5 | 39.5
Heat vs Delta T | 7.0656 | 9.4866 | 12.0491 | 14.4813 | 17.1499 | 19.8986 | 22.5516 | 25.6106 | 28.1846 | 31.0857
Power [W]
Temperature [K]
Chart: 
| 92420.11222874805 | 101505.6837636103 | 108232.4587878528 | 109469.4827872943 | 115404.1195905976 | 120149.5997951881 | 140242.0201387021 | 135890.7720601114 | 142780.6839170771 | 148556.1455925952
Temperature vs Condutance | 105.4825 | 112.785 | 120.975 | 129.455 | 137.4175 | 145.785 | 154.51 | 162.6125 | 171.0975 | 179.225
Temperature [K]
Heat transfer coefficient [W/K m2]

## Slide 20: Results: Cu-Cu
This compares with our experimental value of 108232 for the temperature ~120 K, around 6,5 times higher.
For:
Plastic: Modified CMY Model
Comparison between data obtained and a theoretical model.

## Slide 21: Results: Al-Al
Chart: 
| 0.0 | 50.0 | 100.0
Teste 1A | 130 | 120.2 | 109.9
Teste 1B | 100 | 90.8 | 81.8
Teste 2A | 147.6 | 134.3 | 120.4
Teste 2B | 107.3 | 95 | 82.9
Teste 3A | 163.4 | 147.2 | 130.2
Teste 3B | 114.3 | 98.9 | 84.2
Teste 4A | 179.9 | 160.6 | 140.4
Teste 4B | 121.6 | 103.2 | 85.5
Teste 5A | 195.9 | 173.5 | 150.2
Teste 5B | 128.7 | 107.2 | 86.7
Teste 6A | 212.1 | 186.8 | 160.3
Teste 6B | 136.1 | 111.5 | 88
Temperature [K]
Distance [mm]
Extraordinary linearity
Very small difference in extrapolated values
Oxide layer might play a huge role in conductance at the joint
M4 A4-70 Stainless Steel Bolt, (Torque 3 N m)

## Slide 22: Results: Al-Al
Equation | Extrapolated Temperature [K] | Equation | Extrapolated Temperature [K] | Delta T [K] | Mean Joint Temperature [K] | Heat Power [W] | Conductance [W/K] | h [W/K m2]
y = -0,201x + 130,08 | 104,955 | y = -0,182x + 127,27 | 104,52 | 0,435 | 104,7375 | 7,06561 | 16,24278161 | 162427,8161
y = -0,272x + 147,7 | 113,7 | y = -0,244x + 143,87 | 113,37 | 0,33 | 113,535 | 9,48664 | 28,74739394 | 287473,9394
y = -0,332x + 163,53 | 122,03 | y = -0,301x + 159,33 | 121,705 | 0,325 | 121,8675 | 12,04913 | 37,07424615 | 370742,4615
y = -0,395x + 180,05 | 130,675 | y = -0,361x + 175,63 | 130,505 | 0,17 | 130,59 | 14,48128 | 85,184 | 851840
y = -0,457x + 196,05 | 138,925 | y = -0,42x + 191,53 | 139,03 | -0,105 | 138,9775 | 17,14986 | -163,332 | -1633320
y = -0,518x + 212,3 | 147,55 | y = -0,481x + 208,07 | 147,975 | -0,425 | 147,7625 | 19,8986 | -46,82023529 | -468202,3529
y = -0,579x + 228,18 | 155,805 | y = -0,539x + 223,83 | 156,455 | -0,65 | 156,13 | 22,55159 | -34,69475385 | -346947,5385
y = -0,639x + 244,28 | 164,405 | y = -0,6x + 240,27 | 165,27 | -0,865 | 164,8375 | 25,6106 | -29,60763006 | -296076,3006
y = -0,698x + 260,2 | 172,95 | y = -0,659x + 256,43 | 174,075 | -1,125 | 173,5125 | 28,18465 | -25,05302222 | -250530,2222
y = -0,754x + 275,8 | 181,55 | y = -0,718x + 272,53 | 182,78 | -1,23 | 182,165 | 31,08573 | -25,27295122 | -252729,5122
Chart: Power vs Delta T
| 3.355239999999999 | 5.09679 | 6.395200000000001 | 8.041129999999998 | 9.9514 | 11.46686 | 13.53743 | 15.1514 | 16.94896 | 18.58471999999999
 | 9.9 | 13.1 | 15.9 | 18.8 | 21.5 | 24.2 | 26.9 | 29.7 | 32.4 | 35.2
Chart: Mean Temperature vs Condutance
| 162427.8160919531 | 287473.939393941 | 370742.4615384583 | 851839.9999999203 | 1.63332000000016E6 | 468202.3529411952 | 346947.5384615354 | 296076.3005780316 | 250530.2222222222 | 252729.512195124
 | 104.7375 | 113.535 | 121.8675 | 130.59 | 138.9775 | 147.7625 | 156.13 | 164.8375 | 173.5125 | 182.165
Power [W]
Temperature [K]
Temperature [K]
Heat transfer coefficient [W/K m2]

## Slide 23: Results: SS-SS
Chart: 
| 0.0 | 50.0 | 100.0
Teste 1A | 221.4 | 201.3 | 179.8
Teste 1B | 159.4 | 129.2 | 90.4
Teste 2A | 219.7 | 198.4 | 176.6
Teste 2B | 156.6 | 127.4 | 89.9
Teste 3A | 222.6 | 198.6 | 175.6
Teste 3B | 155.4 | 126.6 | 89.6
Teste 4A | 233.1 | 204.4 | 177.9
Teste 4B | 156.4 | 127.1 | 89.8
Teste 5A
Teste 5B
Teste 6A
Teste 6B
Poor linearity in the data obtained.
Experiment should be repeated. (Shield Deformation)
Huge temperature gradients with very small heat input.
(0,5 to 1,5 W)
Very small difference in extrapolated values
Distance [mm]
Temperature [K]
M4 A4-70 Stainless Steel Bolt, (Torque 3 N m)

## Slide 24: Results: Al-Cu
Chart: 
| 0.0 | 50.0 | 100.0
Teste 1A | 129.5 | 116.2 | 103.4
Teste 1B | 93.7 | 87.1 | 81.1
Teste 2A | 144.7 | 127.2 | 110.4
Teste 2B | 97.9 | 89.5 | 81.9
Teste 3A | 164.7 | 142.2 | 120.4
Teste 3B | 104.2 | 93.3 | 83.4
Teste 4A | 184.8 | 157.3 | 130.3
Teste 4B | 110.4 | 97 | 84.9
Teste 5A | 204.3 | 172.1 | 140.3
Teste 5B | 116.8 | 100.9 | 86.4
Teste 6A | 223.6 | 186.6 | 150.2
Teste 6B | 123.3 | 104.8 | 88
Temperature
Distance
M4 A4-70 Stainless Steel Bolt, (Torque 3 N m)

## Slide 25: Results: Al-Cu
Equation | Extrapolated Temp | Equation | Extrapolated Temp. | Delta T | Heat Power | Conductance | h
y = -0,261x + 129,42 | 96,795 | y = -0,126x + 112,5 | 96,75 | 0,045 | 7,06561 | 157,0135556 | 1570135,556
y = -0,343x + 144,58 | 101,705 | y = -0,16x + 121,77 | 101,77 | -0,065 | 9,48664 | -145,9483077 | -1459483,077
y = -0,443x + 164,58 | 109,205 | y = -0,208x + 135,23 | 109,23 | -0,025 | 12,04913 | -481,9652 | -4819652
y = -0,545x + 184,72 | 116,595 | y = -0,255x + 148,43 | 116,555 | 0,04 | 14,48128 | 362,032 | 3620320
y = -0,64x + 204,23 | 124,23 | y = -0,304x + 162,17 | 124,17 | 0,06 | 17,14986 | 285,831 | 2858310
y = -0,734x + 223,5 | 131,75 | y = -0,353x + 175,97 | 131,845 | -0,095 | 19,8986 | -209,4589474 | -2094589,474
Chart: 
| 9.700000000000001 | 12.5 | 16.2 | 19.90000000000001 | 23.50000000000001 | 26.89999999999999
Delta T vs Power | 4.7563 | 5.0968 | 8.7979 | 11.8424 | 13.8338 | 16.5146
Heat Power
Delta T
Variation of extrapolated Delta T insufficient
Same problem faced in Al-AL for the conductance
Cu-AL should also be evaluated

## Slide 26: Discussion/Conclusion
Given the problems faced determining thermal conductivity effectively, it was chosen to develop an empirical approach that could avoid the problem.
An empirical approach is easy to use and understand but will require a complete database able to encompass all the majority of joint designs.
Further testing is required to evaluate the approach for Aluminum and Stainless Steel.
Results for Copper validate this approach, at least, for this material.

## Slide 27: Discussion/Conclusion
Further testing: Reduce the overlap area of the contact joints. (See if it solves the problem with Al tests and SS 304.
Considerer a method to exact evaluating of the contact area. (I suggest dying liquid).
For the case considerer: M4 bolt, the value of 50% tightening torque (2 Nm) plastified the plates materials in the case of Cu and Al. This can make it hard to develop a database in function of tightening torque.

## Slide 28
Thank you for your attention

## Slide 29: FAQ
PT100 Overlap
Contact Area
Plates Deformation
Heating Elements
PT100 Fixation
Radiation Shield
Leak Testing

## Slide 30: PT100 Overlap
Second degree equation for hot part, linear for cold part.
(Copper OFE)

## Slide 31: Contact Area

## Slide 32: Contact Area

## Slide 33: Plates Deformation

## Slide 34: Heating Elements
PTC heating element with self-regulation housed in a compact flat aluminum alloy construction, allowing heat transmission to the thermal medium. This means that no thermal cut-out or thermostat is required.
Length | 40 mm
Width | 35 mm
Height | 8.5 mm
Thermal Power | 50 W
Surface Temperature | 100 º C
Voltage | 12 V ac - 24 V dc
Technical Characteristics:
From practical testing it was determined that they cannot operate bellow ~130 K. Bellow this point the resistance of the heating element becomes to high to allow any current to flow, effectively stopping any electrical heat dissipation.

## Slide 35: Wiring
Copper OFE
180 mm length plate
40 mm from heater
40 mm from heat sink
50 mm x 50 mm overlap joint
0,22 mm copper wire
Distance | Probe | Reading
0 | 1 | 92.0
25 | 2 | 91.3
50 | 3 | 88.8
100 | 4 | 84.9
125 | 5 | 83.9
150 | 6 | 82.8
Copper OFE
200 mm length plate
10 mm from heater
10 mm from heat sink
50 mm x 50 mm overlap joint
0,12 mm manganin wire
Distance | Probe | Reading
0 | 1 | 78.7
50 | 2 | 79.6
100 | 3 | 79.1
150 | 4 | 77.9
200 | 5 | 77.3
250 | 6 | 77.5

## Slide 36: PT100 Fixation

## Slide 37: PT100 Fixation

## Slide 38: Radiation Shield

## Slide 39: Leak Testing