## Slide 1: High Voltage Plugs for feeders instrumentation lines
Jean-Philippe Tock on behalf of
A Bastard, S Clement, P Cruikshank, N Dalexandro, JB Deschamps, R Gauthier, A Grimaud*, A Jacquemod, C Jarrige*
+ Students, industrial partners
CERN
*Consortium Air Liquide Cryogenic Service / 40-30

## Slide 2: Outline
Framework / CERN experience
Cables considered
Integrability of a multi-cable plugs (#15) Cable porosity
Single cable plug
  Cable
  Design
  Manufacturing
  Tests
On-going and further work (for IO)
Conclusions

## Slide 3: Framework
Implementing Agreement 6 (Jan-2010) 0.35 ppy
Implementing Agreement 9 (2011) Task 6 0.5 ppy
Implementing Agreement 13 (2012) Task II.1 0.25 ppy
  Use CERN experience Total resources : 1.1 ppy equivalent (including material, industrial support, …)

## Slide 4: Framework
Implementing Agreement 13 (2012) Task II.1
Part II Task 1:
Complete the laboratory development and tests of plugs meeting the IO requirements
Write up of the relevant test reports and technical specifications for the handing over to the installation teams. These technical specifications should also include the details for the assembly of plugs within the feeders general assembly strategy
Participation to meetings and reviews related to instrumentation and in particular to those where the general assembly strategy for feeders is discussed
General consultancy on vacuum separators and related composite matters

## Slide 5: CERN experience
Line N plugs
600 A SC cables
Interface on the copper matrix

## Slide 6: CERN experience
DFB lambda plates
Up to 6 kA SC cables
Interface on the copper matrix

## Slide 7: CERN experience
SSS busbars plug
13 kA SC cables
Interface on the copper stabiliser

## Slide 8: Cables considered
2010 : Not final ones but similar to start the work
2010-11 : PVC rods For 15 cables mock-up
2011 : XL-PE For 15 cables prototype
2010-11 : For initial design of single cable plug
2012 :XL-PE For single cable final prototypes (Feb-12) - Last cable (summer 12)

## Slide 9: Integration of a 15-cables plug
Principle
Clamps replaced by bolts to save radial space
Metal seals

## Slide 10: Integration of a 15-cables plug
Cable diameter: 12 mm / Pipe diameter 80 mm
With PVC rods to check concept and integration

## Slide 11: Assembly of first prototype (1/5)
Specific cables were prepared sanding and diameter reduction
Protection of sealing surfaces

## Slide 12: Assembly of first prototype (2/5)
Insertion in compression tooling
Installation of the cables samples
For in-situ assembly, tooling will have to be done in 2 halves (half shells)
In-situ installation along the cable length (5-10 m.) will be more tricky

## Slide 13: Assembly of first prototype (3/5)
Preparation of the glue
Vacuum treatment to remove air bubbles
Delicate activity ; specific in-situ procedures and tooling will have to be developed and qualified

## Slide 14: Assembly of first prototype (4/5)
Glue injection
Specific in-situ procedures and tooling will have to be developed and qualified
Torque to be controlled
Compression tooling

## Slide 15: Assembly of first prototype (5/5)
Capping of the cables
Not to be done for installation in ITER because cables extremities are equipped with leak tight connectors

## Slide 16: Leak test of first prototype
Revealed several leaks:
  error on the leak test setup (stainless steel flange re-machined)
  sealing surface of the ULTEM piece deformed (corrected/elastomer seal instead of a metal one)
  glue caps leaking (reinforced)
  plugs interfaces (remachined, sand blasting and redone)
After correction of the leaks, the repeated test identified the cable itself as a source of leak (porous outer layer) [See next slide]
  Used VACSEAL to make it leak tight but no improvement
Complete encapsulation of one side with ECCOBOND
  Leak tight ! But not conclusive ! for the plug tightness This mainly proves that test setup is working well
It is possible to integrate 15 12-mm cables in a diameter of 80 mm

## Slide 17: Cable porosity
Cable is porous = Helium permeable (XL-PE of AXON)
Bidirectional tests
Compatible with ITER operating scenarios
Q = (K.P.A)/t where: K = permeability,
P = pressure difference,
A= surface,
t = thickness
K = 8 10-11 mbar l cm/cm2 mbar [Aurum]
Q = 3.4 10-4 mbar l/s m
For XL-PE: Estimate of 5 10-5 mbar l/s m (large uncertainty)

## Slide 18: Single cable plug : The cable XL-PE (AXON)
Metrological measurement
Adhesion tests
  Room temperature
  After LN2 shocks
Average diameter : ≈ 12 mm
Max = 12.57 mm / min =11.53 mm

## Slide 19: Single cable plug : Design
Sanded and stripped
ULTEM :Polyetherimide (PEI) Used at CERN and qualified
Eccobond 286A

## Slide 20: Single cable plug : Manufacturing
Cable stripping
Original goal was to save on diameter (Not useful with new design)
Provides mechanical fixation
Due to porosity of the outside layer, provides better sealing (see results of cut later)
Procedure and criteria have been defined
  Thermal stripper / Pictures for acceptance criteria

## Slide 21: Single cable plug : Manufacturing
Cable preparation

## Slide 22: Single cable plug : Manufacturing
Cable preparation

## Slide 23: Single cable plug : Manufacturing
Plug assembly

## Slide 24: Single cable plug : Manufacturing
Procedure
Single cable plug procedure defined by CERN
Adapted by IO for prototype plugs

## Slide 25: Single cable plug : Prototypes
 | Sanded | Stripped
Time | J | K
Cost | J | K
In-situ assembly | J | K
Mech fixation | K | J
Leak rate | K | J
Reproducibility | ? | ?
Stripped variant is preferred for better leak tightness
The in-situ assembly procedure will be delicate
Matrix thickness does not influence performance
Recommend to develop mock-ups and train the technicians

## Slide 26: Single cable plug : Prototypes
Force Controlled Assembly

## Slide 27: Leak test results (1/2)
At manufacturing, all plugs < 10-5 mbar l/s
Degradation occurs in the first (two cycles)

## Slide 28: Leak test results (2/2)
Stripped plugs are performing better than sanded ones
After 2 cycles, the leak rates are stable within a decade (Demonstrated from 10-5 to 10-1 mbar l/s)
Updated 10.12.2012

## Slide 29
PLUGS OBSERVATIONS AFTER CUTTING
Objective: Cutting plugs to observe the glue distribution between the jacket, the inserts and the Ultem matrix.
Procedure: Plugs are cut using a slitting saw then observations are carried out with a Leica microscope in the materials laboratory
Plug 2P
Important thickness variation of the outer jacket
Ultem-Ultem interface seems to be free of defect
Microscopic observations

## Slide 30
PLUGS OBSERVATIONS AFTER CUTTING
Plug 2D
The braid is perfectly immersed into the glue
There is an important thickness variation of the outer jacket (x2), generating a thickness variation of glue around the braid
All the space between the insert and the cable is completely filled with glue
Some glue is also entered into the braid under the outer jacket (migration of the excess glue during the mounting of the plug)

## Slide 31: X-ray
Radiography was tried as an inspection method (QA) but not conclusive for gluing, could be to check the shielding state

## Slide 32: Last CERN activities
3D model of a 15 cables plug
Basic test on the last cable (OK)

## Slide 33: Work performed by IO
Adaptation of procedure to multi-cable plug
Adaptation to the final HV instrumentation cable

## Slide 34: Further work for IO
Technology transfer to an industrial company
  Strict qualification procedure
  Assembly procedure adapted to in-situ assembly
  Representative mock-ups
  Selection of the contractor based on qualification criteria
  Training
Definition of repair and disassembly procedures
Contracts follow-up

## Slide 35: Conclusions
All tasks defined in the agreement have been achieved
A procedure was defined and validated for a single cable plug
  Extra work is required to adapt it to:
    In-situ assembly
    Final cable
    2-7-8 cables
  Disassembly and repair procedures are recommended (Spare cables to be included if possible)
The single cable plug prototypes (#6) performance is compatible with the ITER operation scenarios

## Slide 36
Thank you for your attention and for the open and fruitful working atmosphere during this collaboration, key to achieve the results presented here

## Slide 37: Back-up slides

## Slide 38: Back-up slides
Previous versions

## Slide 39: Single cable plug : Leak tests
Two test methods: Why is it different?
Chart: Plug 1D
| 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7
Helium aspersion | 2e-09 | 1.2e-06
Helium pocket | 2e-09 | 2e-05 | 1.1e-05 | 0.0001 | 5e-06 | 8e-06 | 4.3e-06 | 1.9e-06
Reversed Helium pocket | 1e-06 | 0.011 | 0.003 | 0.0033
The best result is representative

## Slide 40: Back-up slides
Simplified scheme

## Slide 41: Back-up slides
Start adding text here
  First sub-point
    Second subpoint
      Third subpoint
        Fourth subpoint

## Slide 42
Start adding text here
  First sub-point
    Second subpoint
      Third subpoint
        Fourth subpoint